## Slide 1: Bamboo as Construction Materials

## Slide 2
Bamboo is one of the most common materials in construction. It is really easy and fast to grow. They are capable of growing 60 cm or more per day
Bamboo is a renewable and versatile resource, characterized by high strength and low weight, and is easily worked using simple tools

## Slide 3: ADVANTAGES
Low-cost and environment friendly.
Light weight compared to steel.
Shock absorbing and thus earthquake resistant.
It uses less fossil fuel to manufacture.
Bamboo can prevent pollution by absorbing large amounts of nitrogen from waste water and reducing the amount of carbon dioxide in the air.
Its abundance in tropical and subtropical regions makes it an economically advantageous material.

## Slide 4: DISADVANTAGES
It is not that uniform, i.e., large varieties of bamboo are found having different tensile strength.
It has tendency to absorb water and also to release water on drying.
Bamboo is easily infected by wood-boring insects and attracts living organisms, such as, fungi and insects because of its high content of nutrients unless treated with wood preservatives or kept very dry.
Need some treatment for presevation
Less durability than steel
It is susceptible to catch fire as compared to steel.

## Slide 5: BASIC PROPERTIES OF BAMBOO
TENSILE STRENGTH
COMPRESSIVE STRENGTH
ELASTIC MODULUS
ANISOTROPIC PROPERTIES
SHRINKAGE
FIRE RESISTANCE

## Slide 6: TENSIL STRESS AND UNIT WEIGHT
The common tensile stress in steel reinforcement is 160 N/mm2 and in bamboo 370 N/mm2.
The mass per volume of steel is 7850 kg/m3 and of bamboo is about 400-600 kg/m3.
Evidently bamboo will be cheaper because the price of bamboo per weight will be less than half that of steel.

## Slide 7: MODULUS OF ELASTICITY
The cellulose fibers in bamboo act as reinforcement similar to reinforcing steel bars in concrete. The distribution of these fibers increases from the inside to the outside.
The E-modulus for bamboo is about 70 000 N/mm2 – 100 000 N/mm2 and about 50% of the cross-section of the fiber is cellulose; the E of the fiber is 35 000 N/mm2.
In most bamboos, fibers constitute about 60% on the outside and 10% on the inside.

## Slide 10: DURABILTY
Bamboo with low humidity is less prone to mould attacks especially when humidity content is less than 15%.
Physical and mechanical properties of bamboo increase with a decrease in its humidity content.
Bamboo to be treated with a preservative needs to be dry to facilitate penetration. Bamboo can be dried in air, green house, and oven or by fire

## Slide 11: PRESERVATION OF BAMBOO
NON CHEMICAL METHODS OR TRADITIONAL METHOD
CHEMICAL METHODS

## Slide 12: Traditional preservation
Various ways of preserving bamboo include:
Cutting time control.
the timing of bamboo cutting
Bamboo soaking.
Bamboo that has been cut down is soaked for months or even years so that it is resistant to weathering and pest attacks. Immersion is done either in ponds, rice fields, ditches, rivers or in the sea. The disadvantage of this system is that bamboo that is soaked for a long time, when removed will emit mud and an unpleasant odor, it will take a long time after soaking to dry until the odor is reduced and can be used as building material.

## Slide 13
Bamboo fumigation.
Traditionally, bamboo is also sometimes smoked to increase its durability. Traditionally bamboo is placed in a smoky place (kitchen or other burning place), gradually reducing the humidity of bamboo so that biological damage can be avoided.
Dyeing with lime.
Bamboo in the form of splits or wedges is dipped in a solution of lime (CaOH2) which then turns into calcium carbonate which can block water absorption so that the bamboo is protected from fungal attacks.
Grilling/burning/heating.
Usually for bamboo with a small diameter such as the "cendani" type. Heating can increase the resistance of bamboo and make it more aesthetically pleasing, the color of bamboo becomes more yellow and shiny. In large diameter bamboo, heating is usually done to straighten bent bamboo or vice versa. The process of heating bamboo can damage the sugar structure in bamboo, thus forming carbon, as a result, bamboo that has been heated or burned is not liked by beetles or fungi and avoids damage.

## Slide 14
Chemical Preservatives Recommended
Coal Tar Creosote
Copper – chrome - arsenic compositions
Acid- cupric – chromate composition
Copper – chrome- born composition
Copper zinc – napthanate Abietates

## Slide 15
Process of Preservation
IS 401:2001 Code of Practice for Preservation of Timber
1. Surface application ( brushing, dipping)
2. Hot & Cold Method
3. Boucheire Process
5. Inter Nodal Injection
4. Diffusion Process

## Slide 16: Bamboo Application for Building

## Slide 17: Bamboo can be used to make all building components, both structural and non-structural.
a) Bamboo Foundation
b) Bambu as Slab reinforcement

## Slide 18
c) Bamboo as wall reinforcement
d) Bamboo as roof structure

## Slide 19
c) Scaffolding
d) Bamboo reinforcement

## Slide 20: Bamboo reinforcement

## Slide 21: GREEN SCHOOL BUILDING
Heart of Green School,
interior designed radially with column center,

## Slide 22
Struktur atap spiral membuat cahaya siang hari mudah masuk,

## Slide 23
Gambar Mepantigan Hall
Gambar Konstruksi Mepantigan

## Slide 24
Gambar Keunikan
Struktur Heart of Green
School

## Slide 25: Ground improvement

## Slide 26
For:
Embankment with limited height
Embankment in submerge area
Embankment with tolerable settlement
Embankment in remote area

## Slide 27
Durability?
Bamboo is durable
as long as it is always saturated
Appropriate for embankment in
coastal and swampy area where
it is always saturated

## Slide 30: SEKIAN DAN TERIMAKASIH